Dynamic-Mechanical Properties of Polymers

Michael Hess

Department of Physical Chemistry, University Duisburg-Essen, Campus Duisburg, Duisburg, Germany

Department of Polymer Engineering & Science, Chosun University, KwangJu, South Korea

Department of Materials Science, University of North Texas, Denton, Texas, USA

2. EXAMPLES

Most of the examples by courtesy of Kevin Menard (University of North Texas, Department of Materials Science and Perkin Elmer Corp.)

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Left: silicon rubber with a glass transition at –117°C  and  a melting transition at –40°C. Beyond the melting temperature this crosslinked  (vulcanised) material shows rubber-elasticity with modulus that increases with the temperature.

Right: also a silicone rubber that contains silicone oil  as diluent, as plasticizer.  The oil causes a stress-relaxation at the beginning of the melting transition around –47°C.

R. Kosfeld, M. Hess, Progr. Colloid & Polymer Sci. 66 (1979) 43-50

right figure after  J. K. Gillham, Encyclop. Polym. Sci. Technol. (1986) 2nd ed.; J. K. Gillham, Polym. Eng. Sci. (1979) 19, 676

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

# Text boxes

(b)

(a)

Peak E” = 136.7 °C

Onset E” = 127.3 °C

Onset Tan  = 130.0 °C

Peak Tan = 140.5°C

Onset E’ = 133.1 °C

Tan 

Modulus/Pa

Temperature/C

J/g)

Heat flow/mW

Temperature /C

Inflection Point

(Cp

Tf

Onset

Tg by DMA and DSC

This Tg is normally undetectable in the DSC!!!!!! Because the step in cp is broad

and flat (hindered mobility by crosslinking)

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Transitions are clearly seen in highly crosslinked samples

Polymer  A

Temperature/K

E’

E’

Polymer  B

+

=

E’

Temperature/K

Both Tgs

Block Copolymers

Graft Copolymers

Immiscible Blends

Random

Copolymers &

Miscible Blends

E’

Single Tg

Exact T depends on

concentration of A and B

Temperature/K

Temperature/K

Blends and Copolymers

T*

Tg or

Alpha

For example, crystal-crystals slips can cause transitions

It’s not always so simple:

DSC

DMTA

Tm

Cold Crystallization

Tg

Cold Crystallization in PET

Impact was good if Tg/T was 3 or less.

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Poor

Good Impact Strength

Tg

Transitions

#### Dissipation of mechanical energy:

#### Higher Order Transitions affect toughness

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton

Kevin P. Menard, Dynamic-Mechanical Analysis, CRC-Press (1999) Boca Raton